Classification of visual quality of block Mica

The Classification of the visual quality of natural muscovite block mica shall fall into the following twelve categories: -

| ASTM Visual Quality | Commercial Designation |
| --- | --- |
| V-1 | Clear |
| V-2 | Clear and Slightly Stained |
| V-3 | Fair Stained |
| V-4 | Good Stained |
| V-5 | Stained A Quality |
| V-6 | Stained B Quality |
| V-7 | Heavy Stained |
| V-7A | Densely Stained |
| V-8 | Black Dotted |
| V-9 | Black Spotted |
| V-10 | Black Stained |
| V-10A | Densely Black and Red Stained |

ASTM GRADE SIZES OF MUSCOVITE UNCUT MICA FILMS AND BLOCKS

| ASTM Grade (sizes) | AREA OF MINIMUM RECTANGLE |  | MINIMUM DIMENSION OF ONE SIDE |  |
| --- | --- | --- | --- | --- |
|  | SQ. IN. | EQUIVALENT SQ. CM. | IN. | EQUIVALENT CM. |
| OOEE SPECIAL | 100 | 650 | 4 | 10 |
| OEE SPECIAL | 80 | 520 | 4 | 10 |
| EE SPECIAL | 60 | 390 | 4 | 10 |
| E SPECIAL | 48 | 310 | 4 | 10 |
| A.1(SPECIAL) | 36 | 235 | 3.5 | 8.8 |
| NO. 1 | 24 | 155 | 3 | 7.6 |
| NO. 2 | 15 | 97 | 2 | 5.0 |
| NO. 3 | 10 | 65 | 2 | 5.0 |
| NO. 4 | 6 | 40 | 1.5 | 3.8 |
| NO. 5 | 3 | 20 | 1 | 2.5 |
| NO. 5.5 | 2.5 | 15 | 7/8 | 2.2 |
| NO. 6 | 1 | 6.5 | ¾ | 1.9 |